## Slide 1
Material Science & Engg.
BME303
Module-2
Physical Metallurgy
Prof. DEVARAJ M R
Associate professor,
Dept. of Mechanical Engineering,
ATMECE, Mysuru

## Slide 2
COMMON ALLOY STEELS
Steel can be classified in several ways. Some of them are according to:
Carbon Content:
Low carbon
Medium carbon
High carbon steels.
II. a. Hypo-eutectoid steels (˂0.8%C)
b. Hyper-eutectoid Steels (˃0.8%C)
Method of Manufacture:
1. Bessemer Steel
2. Open Hearth Steel
3. Electric Furnace steel
4. Crucible steel etc.,

## Slide 3
III. Based on Application of Steel:
Machine Steel
Spring Steel
Boiler Steel
Structural Steel
Tool Steel etc.
IV. Chemical Composition:
(a). Plain carbon steel and (b). Alloy Steels.
Standard Institutions:
AISI- American Iron and Steel Institute
BIS- Bureau of Indian Standards
SAE- Society of Automotive Engineers.
American society for Testing and Materials
The above institutions have classified steels also according to chemical composition.

## Slide 4
For convenience, we have to study the different types of steels classified according to their chemical composition, i.e., Plain Carbon steels and Alloy Steels
Plain Carbon Steels
Plain carbon steels can be classified once again according to the percentage of carbon,
Low carbon steel- up to 0.25% carbon
Medium carbon steel- 0.25% to 0.55% carbon
High carbon steel- above 0.55%carbon.
Generally, Plain carbon steels contains iron and carbon, and always come with traces of
Sulphur and phosphorous and also sometimes small quantities of silicon and manganese.

## Slide 5
Low Carbon Steels
Of all the different kinds of steels, those produced in the greatest quantities are low carbon steels.
The Characteristics of low carbon steels are:
Composition:-- up to 0.25%C
Microstructure:-- Predominantly α-Ferrite and small quantities of Pearlite.
Properties:--Relatively soft and weak but out standing ductility and toughness.
They possess very good Machinability and weldability.
Example: Mild Steel
Advantages: Least expensive to Produce.
Dis-advantages: Unresponsive to hardening heat treatment because martensite difficult to form owing to very low carbon content.
Strengthening can be accomplished only by cold work. Very low hardenability.

## Slide 6
Medium Carbon Steels
Composition: From 0.25% to 0.55%C
Microstructure: α-Ferrite and Pearlite
Properties: Stronger than Low carbon steel but less tougher than it.
Advantages: Best range for adding alloying elements. Good mix of strength and ductility.
Applications: Railway wheels and Tracks, gears, crank shafts and other machine parts.

## Slide 7
High Carbon Steels
Composition: From 0.55% up to 2.1%C
Microstructure: Cementite (Fe3C) and Pearlite (when C˃0.8%).
Α-ferrite and Pearlite (when C˂0.8%)
Properties: Hardest, Strongest least ductile when compared with Low and medium carbon steels.
Advantages: Best range to make tool steels.
Dis-advantages: cannot be used for operations where ductility and Malleability are required.
Applications: Knives, Razors, hack-saw blades, high strength wires etc.

## Slide 8
ALLOY STEELS
Steels which acquire some characteristic properties due to the addition of alloying elements other than carbon, are known as alloy steels. Alloying elements are added to steels for many purposes. Some of the reasons are:
Increase hardenability.
Improve strength at ordinary temperatures.
Improve wear and corrosion resistances.
Improve mechanical properties at either high or low temperature.
Improve toughness without greatly sacrificing strength.

## Slide 9
Effect of Alloying Elements on Steel
Alloying elements that are added to steel may be classified according to the way they affect the principal phases of steel, i.e., α-ferrite, Cementite (Fe3C) (Iron carbide) and austinite.
Elements which tend to form carbides: These elements combine with carbon to form carbides just like Iron forms iron carbide (Fe3C). These carbides tremendously increase the hardness and wear resistance of the steels but at the same time render them brittle.
Example: Chromium, Tungsten, titanium, Vanadium, molybdenum, Manganese, etc.
2. Elements which tend to graphitize carbon:
These elements when added to steels oppose the formation of carbides where carbon is in the combined form but instead stabilizes carbon to occur in its free form as graphite.
Example: silicon, cobalt, aluminum, Nickel etc.

## Slide 10
4. Elements which tend to stabilize ferrite:
These elements are more soluble in α- iron than in γ-iron. Hence they are ferrite stabilizers.
Example: Chromium, Tungsten, Molybdenum, silicon etc.
3. Elements which tends to stabilize austinite:
These elements when added lowers the A3 temperatures and raises the peritectic point, thereby increasing the range in which austinite is stable.
Some of the elements appear in more than one group and it means that they have more than one effect.

## Slide 11
Types of Alloy Steels
Alloy Steels may be divided into four classes:
Structural steels
Tool and Die steels
Magnetic alloys
Stainless and heat-resisting steels