## Slide 1
Material Science & Engg.
BME303
Module-2
Physical Metallurgy
Prof. DEVARAJ M R
Associate professor,
Dept. of Mechanical Engineering,
ATMECE, Mysuru

## Slide 2
Physical Metallurgy
Alloy Systems: Classification of Solid solutions, Hume- Rothery Rules
Diffusion: Diffusion Mechanisms: Vacancy Diffusion and Interstitial Diffusion, Fick’s laws of diffusion, Factors affecting diffusion.
Phase Diagrams: Gibbs Phase Rule, Solubility limit, phase equilibrium and Phase Diagrams: Isomorphous systems, Invariant Binary Reactions: Eutectic reaction, Eutectoid reaction and Peritectic reaction, Lever Rule, Iron-Carbon Diagram. Effect of common alloying elements in steel.
Numerical on Lever rule.
MODULE-2

## Slide 3
Solid Solution
When two metals are mixed together, they form an alloy if one metal is soluble in the other one in solid state. Therefore, an alloy is a solid solution of two or more metals.
Solid solution is a combination of two metals which are completely soluble in both the solid and liquid states.
Solid solution is a phase, where two or more elements are completely soluble in each other. Depending on the ratio of the solvent (matrix) metal atom size and solute element atom size, two types of solid solutions may be formed: substitution or interstitial.

## Slide 4
The term solid solution is used just as liquid solution, because the solute and solvent atoms (applying the term solvent to the element in excess) are arranged in random.
The difference between a solid and liquid solution is that, in solid solution, the size of the solute atoms greatly affect the solubility of the element which is of little consequence I liquid solutions.
The solid solubility of one metal in another depends on a number of factor a set of rules were formulated and these are usually called the Hume-Rothery rules.

## Slide 5
Primarily there are two types of solid solutions -
Substitutional – Solute atoms occupy the regular lattice sites of the parent metal (solvent). Substitutional solid solutions can be random (Cu-Ni) or ordered (Cu-Au) and Au-Ag and Cu-Ag.
Interstitial – Solute atoms occupy the interstitial positions (Steel – C solute atoms in Fe)

## Slide 6
Substitutional
Solute atoms replace solvent atoms.
It can be formed with limited solubility
e.g. Bronze (Sn in Cu)
or unlimited solubility e.g. Brass (Zn in Cu), in this case both atoms have nearly the same size.
2) Interstitial solid solutions
Small atoms located at the interstices between larger atoms. E.g. C in Fe
3) Ordered solid solutions
The two types of atoms arranged in a specific order.
Heating always destroys the ordering in the solution.

## Slide 8
Interstitial solid solutions

## Slide 9
In brief these rules (Hume-Rothery rules) are as follows:
Crystal structure
The atomic size factor
The electrochemical effect
Relative valence factor
Electro-negativity
Solid solutions, in accordance with the Hume-Rothery rules, may form if the solute and solvent have:
Similar atomic radii (15% or less difference)
Same crystal structure
Similar electronegativities
Similar valency

## Slide 13
Phase
A phase can be defined as a physically distinct and chemically homogeneous portion of a system having its own boundry, that has a particular chemical composition and structure.
A solid phase has its own crystal structure and its set of individual properties.
Example: α-Ferrite, Fe3C, Austinite and homogenous liquid etc.
Water in liquid or vapor state is single phase. Ice floating on water is an example two phase system.

## Slide 14
Phases:
A phase is a homogenous, physically distinct and mechanically separable portion of the material with a given chemical composition and structure.

## Slide 15
Component
– is either pure metal and/or compounds of which an alloy is composed. The components of a system may be elements, ions or compounds. They refer to the independent chemical species that comprise the system.
Components:
The elements or compounds that are mixed initially (Al and Cu).
System
– it can either refer to a specific body of material under consideration or it may relate to the series of possible alloys consisting of the same components but without regard to alloy composition.

## Slide 16
Terminology

## Slide 17
A phase diagram is essentially a graphical representation of an alloy system.
Phase diagrams are also called as equilibrium diagrams or constructional diagrams.
Phase diagrams are classified as:
          Unary Phase diagram
          Binary Phase diagram
          Ternary Phase diagram
  Unary Phase diagram is nothing but the Pressure-Temperature diagram of a pure metal.

## Slide 18
  Unary Phase diagram

## Slide 21
The Nature and occurrences of these phases in turn is a function of different independent variables such as temperature, pressure and composition.
So in order to predict the properties of materials,
it is important to know the following:
The conditions under which different phases exist.
The conditions under which a change of phase will occur.
Therefore phase diagrams are constructed to provide the following information.

## Slide 22
Therefore phase diagrams are constructed to provide the following information.
The different phases existing in the alloy for any combination of temperature and composition.
(Pressure is assumed to be constant at atmospheric value.)
Temperature at which different compositions begin and end solidification.
To study and control process such as solidification and heat treatment of metals and alloys.
A phase diagram is essentially a graphical representation of an alloy system.
Phase diagrams are also called as equilibrium diagrams or constructional diagrams.

## Slide 23: Classification of Binary Phase Diagrams All binary phase diagrams can be classified according to the appearance of the following reactions or Transformations in them. These include:
Solid solution or Isomorphous phase diagram
Eutectic system(Eutectic type phase diagram)
Eutectoid transformation
Peritectic reaction
Peritectoid transformation

## Slide 24: Solid solution or Isomorphous phase diagram
Solid solution is a combination of two metals which are completely soluble in both the solid and liquid states

## Slide 25
Thank You