## Slide 1
Introduction to Non-Traditional Machining
BME755A
Ultrasonic Machining (USM)
Mr. Hemanth B R
Assistant Professor,
Dept. of Mechanical Engineering,
ATMECE, Mysuru

## Slide 2
Module 2
Ultrasonic Machining (USM):
Introduction, Equipment and material process
Effect of process parameters: Effect of amplitude and frequency, Effect of abrasive grain diameter, effect of slurry, tool & work material.
Process characteristics: Material removal rate, tool wear, accuracy, surface finish
Applications, advantages & limitations of USM.
Abrasive Jet Machining (AJM):
Introduction, Equipment and process of material removal,
Process variables: carrier gas, type of abrasive, work material, stand-off distance (SOD).
Process characteristics-Material removal rate, Nozzle wear, accuracy & surface finish.
Applications, advantages &limitations of AJM.

## Slide 3
COURSE OUTCOME
DESCRIBE THE CONSTRUCTIONAL FEATURES, PERFORMANCE PARAMETERS, PROCESS CHARACTERISTICS, APPLICATIONS, ADVANTAGES AND LIMITATIONS OF USM & AJM

## Slide 4
ABRASIVE PARTICLES

## Slide 5
The abrasive slurry is a mixture of abrasive material (e.g. silicon carbide and boron carbide) suspended in water or oil.
SLURRY
Abrasive slurry Slurry foamed Foam application

## Slide 6
Principle of Ultrasonic machining
In the process of Ultrasonic Machining, material is removed by micro-chipping or erosion with abrasive particles.
In USM process, the tool, made of softer material than that of the workpiece, is oscillated by the Booster and Sonotrode at a frequency of about 20 kHz with an amplitude of about 25.4 um (0.001 in).
The tool forces the abrasive grits, in the gap between the tool and the workpiece, to impact normally and successively on the work surface, thereby machining the work surface.
During one strike, the tool moves down from its most upper remote position with a starting speed at zero, then it speeds up to finally reach the maximum speed at the mean position.

## Slide 7
Equipment of Ultrasonic machining
The process is performed by a cutting tool, which oscillates at high frequency, typically 20-40 kHz, in abrasive slurry.
The tool is gradually fed with a uniform force.
The high-speed reciprocations of the tool drive the abrasive grains across a small gap against the workpiece.
The impact of the abrasive is the energy principally responsible for material removal in the form of small wear particles that are carried away by the abrasive slurry.
The shape of the tool corresponds to the shape to be produced in the workpiece

## Slide 8
Equipment of Ultrasonic machining
The process is performed by a cutting tool, which oscillates at high frequency, typically 20-40 kHz, in abrasive slurry.
The tool is gradually fed with a uniform force.
The high-speed reciprocations of the tool drive the abrasive grains across a small gap against the workpiece.
The impact of the abrasive is the energy principally responsible for material removal in the form of small wear particles that are carried away by the abrasive slurry.
The shape of the tool corresponds to the shape to be produced in the workpiece

## Slide 9
Transducer
• Piezoelectric transducers utilize crystals like quartz whose dimensions alter when being subjected to electrostatic fields.
• The charge is directionally proportional to the applied voltage.
• To obtain high amplitude vibrations the length of the crystal must be matched to the frequency of the generator which produces resonant conditions.
Components of Ultrasonic machining
Transducer
Tool Holder/ Acoustic Head
Abrasive and Abrasive Slurry
Tool

## Slide 10
Components of Ultrasonic machining
Tool Holder/Acoustic head
• The shape of the tool holder is cylindrical or conical, or a modified cone which helps in magnifying the tool tip vibrations.
• Its function is to increase the tool vibration amplitude and to match the vibrator to the acoustic load. Therefore it must be constructed of a material with good acoustic properties and be highly resistant to fatigue cracking.
• Monel and titanium have good acoustic properties and are often used together with stainless steel, which is cheaper.

## Slide 11
3. Abrasive
• Abrasive Slurry
common types of abrasive
Boron carbide (B4C) good in general, but expensive
Silicon carbide (SiC) glass, germanium, ceramics
Corundum (Al2O3– Aluminium Oxides)
Diamond (used for rubies , etc)
Boron silicon-carbide (10% more abrasive than B4C)
Components of Ultrasonic machining
Liquid
- Water most common
Benzene
Glycerol
Oils
High viscosity decreases MRR

## Slide 12
4. Tool
• Tool material should be tough and ductile. Low carbon steels and stainless steels give good performance.
• Tools are usually 25 mm long ; its size is equal to the hole size minus twice the size of abrasives.
Tool Size = Hole Size – 2(Size of Abrasives)
• Mass of tool should be minimum possible so that it does not absorb the ultrasonic energy.
• It is important to realize that finishing or polishing operations on the tools are sometimes necessary because their surface finish will be reproduced in the workpiece.
• Tool and toolholder are often attached by silver brazing.
Components of Ultrasonic machining

## Slide 13
Machining occurs when the abrasive particles, suspended in the slurry between the tool and workpiece, are struck by the downstroke of the vibration tool.
The impact propels the particles across the cutting gap, hammering them into the surface of both tool and workpiece. Collapse of the cavitation bubbles in the abrasive suspension results in very high local pressures.
Under the action of the associated shock waves on the abrasive particles, micro cracks are generated at the interface of the workpiece – brittle fracture.
The brittle fracture lead to chipping of particles from the workpiece.
Mechanism of Metal Removal in Ultrasonic machining

## Slide 14
Tool feed mechanism

## Slide 15
Effect of Abrasive Grain
Effect of parameters (Variables) of USM
01
02
03
04
05
06
Effect of Amplitude & Frequency of vibrations
Effect of Applied Static Load
Effect of Work Material
Effect of Tool
Effect of Slurry

## Slide 16
Grain size of the abrasive has a strong influence on the material removal rate & surface finish.
Grain size determines the accuracy of the cavity configuration in USM.
When the grain size becomes comparable to the tool amplitude, a maximum rate of machining is achieved but increase in grain size will reduce the machining rate.
Grain size of 200-400 are used for roughing & 800-1000 for finishing.
Boron Carbide is the fastest cutting abrasive & is commonly used.
Aluminum oxide & silicon carbide are also employed.
Effect of Abrasive Grain

## Slide 17
Effect of Abrasive Grain Diameter

## Slide 18
The metal removal rate or cutting rate increases with increase in both amplitude & vibration of the tool.
The cutting rate increases linearly with an increase in both amplitude and frequency.
However, increasing the amplitude tends to increase the surface roughness, but the effect is minimal.
Effect of Amplitude & Frequency of vibrations
The frequency & amplitude of vibrations ranges from 15-30kHz & 25-100μm respectively.

## Slide 19
Static load is the load or force with which the abrasive particles are initially kept pressed against the workpiece by the tool force before they are accelerated to strike against the w/p during a vibration cycle.
The machining rate reaches a maximum as the static load on the tool is increased.
The surface finish is found to be little affected by the applied static load .
It is observed that higher loads, do not give a rougher finish, In fact surface finish is improved because the grains are crushed to small size with higher loads
Effect of Applied Static Load

## Slide 20
Effect of Slurry
Cutting rate can be increased with an increase in slurry concentration.
It is found that a sharp drop in material removal rate with increasing viscosity.
The pressure with which slurry is fed into the cutting zone has a remarkable effect on the material removal rate.

## Slide 21
The shape of the tool face also affects the cutting rate.
A narrow rectangular tool gives a greater maximum cutting rate than a tool of the same area with a square cross section.
A rise in cutting rate by 50% is seen by replacing a cylindrical tool with a conical cone.
Effect of Tool
Effect of Work Material
Since the cutting forces involved in USM are not large, no mechanical stresses are set up in the work material.
The microstructure of work material is not affected as the temperature generated at the cutting area is not that high.
But if the flow of abrasive slurry is impaired then work material may not finished effectively

## Slide 22
Process Characteristics of Ultrasonic machining
Process capability
USM can Machine work piece harder than 40 HRC to 60 HRC like carbides, ceramics, tungsten glass that cannot be machined by conventional methods
Tolerance range 7 micron to 25 microns
Holes up to 76 micron have been drilled hole depth upto 51mm have been achieved easily. Hole depth of 152mm deep is achieved by special flushing techniques.
Aspect ratio 40:1 has been achieved
Linear material removal rate -0.025 to 25mm/min
Surface finish -0.25 micron to 0.75 micron
Non directional surface texture is possible compared to conventional grinding
Radial over cut may be as low as 1.5 to 4 times the mean abrasive grain size.

## Slide 23
Process Characteristics of Ultrasonic machining

## Slide 24
Machining any materials regardless of their conductivity
USM apply to machining semi-conductor such as silicon, germanium etc.
USM is suitable to precise machining brittle material.
USM does not produce electric, thermal, chemical abnormal surface.
USM can drill circular or non-circular holes in very hard materials
Less stress because of its non-thermal characteristics
Advantages of Ultrasonic machining

## Slide 25
Hard, brittle work materials such as ceramics, glass, and carbides
Also successful on certain metals, such as stainless steel and titanium
Shapes include non-round holes, holes along a curved axis
“Coining operations” - pattern on tool is imparted to a flat work surface
Applications of Ultrasonic machining
Limitations of Ultrasonic machining
USM has low material removal rate. (3-15mm3/min)
Tool wears fast in USM.
Machining area and depth is restraint in USM

## Slide 26
1. Machining of cavities in electrically non-conductive ceramics
2. Used to machine fragile components in which otherwise the scrap rate is high
3. Used for multistep processing for fabricating silicon nitride (Si3N4) turbine blades
4. Large number of holes of small diameter. 930 holes with 0.32mm has been reported ( Benedict, 1973) using hypodermic needles
5. Used for machining hard, brittle metallic alloys, semiconductors, glass, ceramics, carbides etc.
6. Used for machining round, square, irregular shaped holes and surface impressions.
7. Used in machining of dies for wire drawing, punching and blanking operations
Applications of Ultrasonic machining

## Slide 27
8. USM can perform machining operations like drilling, grinding and milling operations on all materials which can be treated suitably with abrasives.
9. USM has been used for piercing of dies and for parting off and blanking operations.
10. USM enables a dentist to drill a hole of any shape on teeth without any pain
11. Ferrites and steel parts , precision mineral stones can be machined using USM
12. USM can be used to cut industrial diamonds
13. USM is used for grinding Quartz, Glass, ceramics
14. Cutting holes with curved or spiral centre lines and cutting threads in glass and mineral or metallic-ceramics
Applications of Ultrasonic machining

## Slide 28
Introduction to Non-Traditional Machining
Abrasive Jet Machining (AJM)
Mr. Hemanth B R
Assistant Professor,
Dept. of Mechanical Engineering,
ATMECE, Mysuru

## Slide 29
DEFINITION:
It is the material removal process where the material is removed by high velocity stream of air/gas or water and abrasive mixture
A focused stream of the abrasive particles, carried by high pressure air or gas is made to impinge on the work surface through a nozzle and work material is removed by erosion by high velocity abrasive particles.
Abrasive Jet machining

## Slide 30
Equipment of Abrasive Jet machining
Equipment
Carrier Gas system
Metering system
AJM nozzle
Abrasives

## Slide 31
Equipment consists of following Main Parts
Nozzle
Abrasive
Carrier gas
Metering system.
Nozzle
A nozzle is used to accelerate the abrasive particles onto the worksurface.
Since the abrasive particles leave the nozzle at a very high velocity, it is subjected to abrasion wear.
The nozzle is made from a hard material like tungsten carbide or synthetic sapphire.
Equipment of Abrasive Jet machining

## Slide 32
It should have excellent flow characteristics.
Re-use of abrasives is not recommended, since the cutting capacity decreases after the first application, and also the chips from the workpiece material combine with abrasives and clog the small orifice in the nozzle.
The mass flow rate of the abrasive particles depends on the pressure and the flow rate of the gas.
Apart from machining, there are certain abrasives like sodium bicarbonate, dolomite, glass etc., used for cleaning, etching, deburring, and polishing operations.
b) Abrasive
Aluminum oxide and silicon carbide are the commonly used
abrasives
The size of the abrasive particle ranges from 10-50 µm
Smaller size abrasives are used for polishing and cleaning,
while the larger ones used for cutting and peening operations.

## Slide 33
C) Carrier gas
Air, nitrogen or carbon dioxide is generally used as a carrier gas.
Air, when used must be to remove moisture, oil and other contaminants before entering the nozzle.
The pressure required is in the range of 2 - 8 kg/cm².
Higher pressure leads to nozzle wear, while lower pressure low metal removal rate.
D) Metering system
The metering system includes mixing chamber, regulator, valves and other devices.
The system must inject an uniform, adjustable flow of abrasive particles into the gas stream.
The amplitude of vibration of the chamber controls the uniform metering of the powder.

## Slide 34
Principle of Abrasive Jet machining
(Mechanism of Material Removal)
• High velocity stream of the abrasives is generated by converting pressure energy of carrier gas or air to its kinetic energy and hence high velocity jet.
• Nozzles directs the abrasive jet in a controlled manner onto workpiece.
Metal cutting action by micro-cutting as well as the brittle fracture of the work material.
Different from conventional sand blasting/shot blasting, finer abrasive grits are used and process or machining parameters are easily controllable.
• Abrasive particles are made to impinge on work material at high velocity.
• Abrasive particles is carried out by carrier gas/air.

## Slide 35
Variables of Abrasive Jet machining:
Abrasive flow rate
Nozzle Tip Distance (NTD) or Stand Off Distance (SOD)
Abrasive Grain Size
Mean Number of Abrasive Particles per Unit Volume of the Carrier Gas
Nozzle Design
Process Parameters of Abrasive Jet machining

## Slide 36
1) Abrasive flow rate velocity:
Increase in the flow rate of abrasives, increases the metal removal rate, because more abrasive particles are available for cutting.
However, when the flow rate exceeds 14 g/min, the abrasive velocity decreases, thereby reducing the metal removal rate.
For the erosion of the worksurface by the abrasives, the minimum jet velocity is found to be 150 m/sec.
The jet velocity is a function of the nozzle pressure, nozzle design, abrasive grain size, and the mean number of abrasives per unit volume of the carrier gas.
Process Parameters of Abrasive Jet machining

## Slide 37
2) Nozzle Tip Distance (NTD) or Stand Off Distance (SOD)
The nozzle tip distance refers to the distance between the tip of the nozzle and the worksurface.
The increase in MRR is maximum up to a distance of about 8 mm; beyond this range, the metal removal rate decreases due to increase in machining area for the same amount of abrasives and decrease in velocity of abrasive particle stream due to drag.
A large NTD leads to poor accuracy of the machined surface.
Process Parameters of Abrasive Jet machining

## Slide 38
3) Abrasive Grain Size
The size of the abrasive grain ranges from 10–50 µm.
An abrasive with larger particle size removes material faster from the worksurface than with the small particle sizes.
Coarse grains are recommended for cutting, while fine grain abrasives for polishing, deburring, etc.
Process Parameters of Abrasive Jet machining

## Slide 39
4) Mean Number of Abrasive Particles per Unit Volume of the Carrier Gas
The mean number of abrasive particles per unit volume of the carrier gas can be obtained from the mixing ratio M, which is defined as, volume flow rate of the abrasive per unit time volume flow rate of the carrier gas per unit time.
A large value of M should result in higher rates of metal removal
However a large abrasive flow rate has been found to adversely influence jet velocity and may sometimes even clog the nozzle.
Thus for a given condition, there is an optimum value of that gives maximum metal removal rate
Process Parameters of Abrasive Jet machining

## Slide 40
5) Nozzle Design
The abrasive particles leave the nozzle at a very high velocity. Thus, it is subjected to abrasion wear.
To overcome this effect, wear resistant materials like tungsten carbide, sapphire, etc, are used for manufacturing nozzles.
Further, the nozzle should be carefully designed so that the pressure loss due to bends, friction, etc., is minimum
Nozzles may be either circular or rectangular in cross section with suitable dimensions
Process Parameters of Abrasive Jet machining

## Slide 41
Effect of Stand of Distance (SOD/NTD)

## Slide 42
Process Parameters of Abrasive Jet machining

## Slide 43
Effect of process parameters on MRR

## Slide 44
Material removal rate – 0.015 cm/min
Narrow slots – 0.12 to 0.25mm ± 0.12mm
Surface finish - 0.25 micron to 1.25 micron
Sharp radius up to 0.2mm is possible
It is possible to cut Steel upto 1.5mm, Glass upto 6.3mm
Machining of thin sectioned hard and brittle materials is possible.
Process Capability of Abrasive Jet machining

## Slide 45
Advantages of AJM
Low capital cost.
Less vibration.
Good for difficult to reach area.
No heat is generated in work piece.
Ability to cut intricate holes of any hardness and brittleness in the material.
Ability to cut fragile, brittle hard and heat sensitive material without damage
Disadvantages of AJM
Low metal removal rate.
Due to stray, cutting accuracy is affected.
Particles is imbedding in work piece and Abrasive powder cannot be reused.

## Slide 46
Abrading/frosting of glass
Cleaning of metallic smears on ceramics, oxides on metals , resistive coating etc.
Manufacture of electronic device, drilling of glass wafers, deburring of plastics, making of nylon and Teflon parts, permanent marking on rubber utensils etc.
Engraving registration numbers on toughened glass used for car windows.
For cutting thin fragile components- Germanium/silicon etc.
For drilling, cutting, deburring, etching and polishing of hard and brittle materials.
Applications of Abrasive Jet machining